## Slide 1: NMF Clustering on X-ray Diffraction Patterns
Abimbola Oluwade | 07/31/2020

## Slide 2: Outline
Background info and work
NMF and methods
Results so far
Future work

## Slide 3: Background
X-ray experiments like those at SSRL help produce XRD patterns for crystal structure identification in materials
Non-negative Matrix Factorization(NMF) is a dimensional reduction and clustering technique used for datasets with positive values like XRD datasets
e.g. Al-Fe-Sn

## Slide 4: Objective
Train computer to divide the materials on the wafer plates into their different clusters
Some clusters could be single, double or triple phased e.g BCC, FCC+BCC, etc
Work with TiNiSn_500C XRD dataset for now
Ground Truth
BCC or BCC+FCC?

## Slide 5: Peripheral Work
First Attempt: Agglomerative Clustering with different distance metrics
Assessment score: average of adjusted mutual info, adjusted rand index, and Fowlkes mallows scores (AMI, ARI & FM scores)
Cosine: 0.799978 Average Diff.: 0.642952 Manhattan: 0.629109
sEuclidean: 0.504296 Euclidean: 0.504296
Ground Truth :1.00
Turns out Alexander had gotten these 

## Slide 6: Why NMF?
NMF has been reported to work well for Al-Li-Fe and Fe-Ga-Pd XRD datasets (Stanev et. al)
Will it improve the assessment score for TiNiSn_500C dataset?
Stanev et. al “Unsupervised phase mapping of X-ray diffraction data by nonnegative matrix factorization integrated with custom Clustering”

## Slide 7: NMF as a dimension reduction technique
NMF is a dimension reduction technique just like Principal Component Analysis (PCA)
However it reduces a matrix V (n_features × m_samples) to 2 matrices: W(n_features×r) and H(r×m_samples).
r is smaller than both n and m hence dimension reduction
Main idea: Find W and H such that

## Slide 8: NMF Solution Implementation
NMF aims to find the best W and H by iteratively updating them until their product is very similar to V starting with random W and H
Frobenius Norm method
Minimize
Update:
Note that updates are done element-wise [i,j] and solution is not unique
(Similar to Euclidean Distance)
Coefficients

## Slide 9: Clustering with NMF/Visualizing W and H matrices
Each column of the W matrix represents 1 distinct phase so r = no. of phases
Each row of the H matrix represents the weight/abundance of each phase in our wafer map
Multiphased region is a cluster

## Slide 10: Procedures
Since r is unknown, try r = 3:11 to obtain many solutions
For each r, check for peak shifting among the r distinct phases
  Pearson Correlation on each pair ≥ [0.7,0.8,0.9]
  Any pair in criteria i. should have same no. of peaks above 2 a.u.
Combine any peak shifted phase(s) found in 2.

## Slide 11: Procedures contd.
At every point, remove any phase contributing ≤ [0.08,0.15,0.25]
At every point, take the 3 most contributing phase if necessary
Plot the wafer map noting that any overlapping phases is a separate cluster (multiphase)

## Slide 12: Results and Observation
The best 4 so far:
      r = 4, Correlation Threshold=0.7, Contribution Threshold= 0.25
      r = 4, Correlation Threshold=0.8, Contribution Threshold = 0.25
      r = 4, Correlation Threshold=0.9, Contribution Threshold = 0.25
      r = 10, Correlation Threshold=0.9, Contribution Threshold = 0.15
Ground Truth:1.00 0.731279 0.731279 0.731279 0.646537
So far the algorithm is not detecting that cluster
Is still not better than Cosine!

## Slide 13: Future Work
Improve Algorithm
  Look into NMFk algorithm to find best r
  Adjust the same peak threshold to account for different max. peaks
Expand dataset
  TiNiSn_600C dataset
  Citrination website

## Slide 14
Q&A